| Englisch: |  |  |  |  |
| --- | --- | --- | --- | --- |
| md = machine direction = längs |  |  |  |
| cd = cross direction = quer |  |  |  |
| top side = Oberseite |  |  |  |  |
| lower side = Unterseite |  |  |  |  |
| Englisch: |  |  |  |  |
| Impregnated special paper |  |  |  |  |
| Impregnated special paper, one-side release coat |  |  |
| Impregnated special paper, one-side coated |  |  |
| Impregnated special paper, double-side coated |  |  |
| Impregnated special nonwoven |  |  |  |
| Technological Data Sheet |  |  |  |
| varitess® 290.150 |  |  |
| Impregnated special nonwoven one-side coated |  |  |
| Variable |  | Test | Unit | Value |
|  |  | Method |  |  |
| Grammage |  | DIN EN ISO 536 | g/m² | 150 |
| Thickness |  | DIN EN ISO 534 | µm | 153 |
| Density |  | DIN EN ISO 534 | g/cm³ | 0,98 |
| Tensile strength | md | DIN EN ISO 1924-2 | N/15 mm | 128 |
|  | cd |  |  | 84 |
| Tensile stretch | md | DIN EN ISO 1924-2 | % | 3,7 |
|  | cd |  |  | 6,4 |
| Wet tensile strength | md | DIN ISO 3781 | N/15 mm | 48 |
|  | cd |  |  | 30 |
| Tear resistance | md | DIN EN 21 974 | mN | 0 |
|  | cd |  |  | 0 |
| Edge tearing resistance | md | ASTM D 1004 | N | 0 |
|  | cd |  |  | 0 |
| Bursting strength |  | DIN EN ISO 2758 | kPa | 0 |
| Bonding strength | md | FL - A 10-011 / 62 | mN | 0 |
|  | cd |  |  | 0 |
| Bending force | md | DIN 53 121, Pkt. 5.1 | mN | 0 |
|  | cd |  |  | 0 |
| Wet elongation (Fenchel) | md | A 10-011 / 27 | % | 0,1 |
|  | cd |  |  | 0,2 |
| Smoothness (Bekk) | top s. | DIN 53 107 | s | 112 |
|  | lower s. |  |  | 31 |
| Water absorption (Cobb) | top s. | DIN EN 20 535 | g/m² | 0 |
|  | lower s. |  |  | 0 |
| Varnishability | top s. | NEN 1836 | 1000/mm | 0 |
|  | lower s. |  |  | 0 |
| Oil absorption (Unger) | top s. | FL - A 10-011 / 80 | g/m² | 0 |
|  | lower s. |  |  | 0 |
| Water repellency time | top s. | FL - A 10-011 / 70 | s | 0 |
|  | lower s. |  |  | 0 |
| Capillary rise |  | FL - DIN ISO 8787 | mm | 0 |
| Air permeability (Bendtsen) |  | DIN 53 120, T.1 | ml/min | 0 |
| Air permeability |  | FL - A 10-011 / 98 | l/m²*s | 0 |
| Whiteness |  | DIN 53 145, T.1 | % | 89 |
| Opacity |  | DIN 53 146 | % | 93 |
| Adhesive strength (RC-side) |  | FL - A 10-011 / 69 | mN/15 mm | 0 |
| Number of double folds | md | Tappi 423 | n | 0 |
|  | cd |  |  | 0 |
| These values are approximate values and do not represent a specification. |  |
| Lahnstein, 02/2007 |  |  |  |  |